## Slide 1: Contactless calliper
15
Martin Marek

## Slide 2: Problem definition
Invent and construct an optical device that uses a laser pointer and allows contactless determination of thickness, refractive index, and other properties of a glass sheet.

## Slide 3: Measuring refractive index using Brewster’s angle

## Slide 4: Measuring the index of refraction: Brewster‘s angle
Fresnel equations → Brewster‘s angle
(reflected beam is completely s-polarized)
Chart: Angle of incidence [˚]
Brewster‘s angle

## Slide 5: Brewster‘s angle in logarithmic scale
Chart: Angle of incidence [˚]

## Slide 6
Apparatus for measuring Brewster‘s angle
Diffraction-limited laser beam
Polarizing filter
CMOS sensor
Glass sheet

## Slide 7
Apparatus for measuring Brewster‘s angle
Mirror-calibrated laser
(to point along a yellow line)

## Slide 8
Apparatus for measuring Brewster‘s angle
Mirror-calibrated camera
(to be situated directly above glass sheet)
Level-calibrated tripod
(to eliminate perspective aberrations)

## Slide 9
Brewster‘s angle measurements

## Slide 10
Brewster‘s angle measurements
Error = 0.15˚

## Slide 11
Brewster‘s angle measurements
Measurements of 7 different sheets

## Slide 12
Chart: Index of refraction of different-width sheets of glass
| 1.0 | 2.0 | 3.0 | 4.0 | 5.0 | 6.0 | 7.0 | 8.0
 | 1.4956 | 1.5692 | 1.5057 | 1.5006 | 1.5328 | 1.5346 | 1.5311
Brewster‘s angle measurements
Sheet 1
Sheet 2
Sheet 3
Sheet 4
Sheet 6
Sheet 7
Sheet 8
zoom

## Slide 13
Chart: Index of refraction of different-width sheets of glass
| 1.0 | 2.0 | 3.0 | 4.0 | 5.0 | 6.0 | 7.0 | 8.0
 | 1.4956 | 1.5692 | 1.5057 | 1.5006 | 1.5328 | 1.5346 | 1.5311
Brewster‘s angle measurements
Sheet 1
Sheet 2
Sheet 3
Sheet 4
Sheet 6
Sheet 7
Sheet 8
All of the sheets are from the same manufacturer
What’s going on?

## Slide 14
Chart: Index of refraction of different-width sheets of glass
| 1.0 | 2.0 | 3.0 | 4.0 | 5.0 | 6.0 | 7.0 | 8.0
 | 1.5096 | 1.5705 | 1.509 | 1.5063 | 1.4949 | 1.523 | 1.5435 | 1.5214
 | 1.4956 | 1.5692 | 1.5057 | 1.5006 | 1.5328 | 1.5346 | 1.5311
Brewster‘s angle: 2nd (verification) measurements
Sheet 1
Sheet 2
Sheet 3
Sheet 4
Sheet 5
Sheet 6
Sheet 7
Sheet 8
error 0.008
✓

## Slide 15: Limitations of reflections method: phase diagram
Chart: Refractive index
Suitable for measurement
Unsuitable for measurement

## Slide 16: Brewster’s angle: conclusion
Usage: | Refractive index
Error: | ± 0.08
Limitation (n = 1.5): | ~0.16mm

## Slide 17: Measuring refractive index using Fresnel equations

## Slide 18: 2nd method of measuring the index of refraction: Intensity of p-polarized reflected light
zoom
Chart: Angle of incidence [˚]

## Slide 19: 2nd method of measuring the index of refraction: Intensity of p-polarized reflected light
Chart: Reflectance of p-polarized light
| 8.261925731320797 | 16.26334830338988 | 25.41433558868151 | 34.1255833836664 | 44.1141527297945 | 48.87906696725079 | 51.98101654510255 | 52.8651428724251 | 56.68856536336511 | 61.49880066796349 | 65.29744512988488
 | 0.041375 | 0.03971 | 0.029278 | 0.023927 | 0.012261 | 0.0062048 | 0.0025265 | 0.0015883 | 0.00012447 | 0.0044942 | 0.013561
 | 0.013304 | 0.0094128 | 0.0063555 | 0.0040174 | 0.0022986 | 0.001112 | 0.00038182 | 4.1942e-05 | 3.4696e-05 | 0.0003098 | 0.00082341 | 0.0015373 | 0.002418 | 0.0034365 | 0.0045675 | 0.0057888 | 0.0070812 | 0.008428 | 0.0098147 | 0.011228 | 0.012659 | 0.014095 | 0.015531 | 0.016957 | 0.01837 | 0.019762 | 0.021129 | 0.022469 | 0.023777 | 0.025051 | 0.026288 | 0.027486 | 0.028645 | 0.029762 | 0.030836 | 0.031866 | 0.032853 | 0.033795 | 0.034691 | 0.035542 | 0.036348 | 0.037107 | 0.037821 | 0.038488 | 0.03911 | 0.039686 | 0.040216 | 0.040701 | 0.04114 | 0.041534
Error caused by non-uniform cross section of intensity of laser beam (we only consider the highest intensity pixel)
Fit values:
Refractive index:

## Slide 20: Limitations of reflections method: phase diagram
Chart: Refractive index
Suitable for measurement
Unsuitable for measurement

## Slide 21: Fresnel equations: conclusion
Usage: | Refractive index
Error: | ± 0.015
Limitation (n = 1.5): | 0.16mm

## Slide 22: Measuring thickness using internal reflections

## Slide 23: Thickness and index of refraction: internal reflection
measured
Obtained by regression
Derived from geometrical optics

## Slide 24: Thickness and index of refraction: internal reflection
measured
Obtained by regression
Derived from geometrical optics
Brewster’s angle

## Slide 25: Thickness and index of refraction: internal reflection
CMOS sensor
1.

## Slide 26: Thickness and index of refraction: internal reflection
Extremely thin beam
2.
Camera
3.
CMOS sensor
1.

## Slide 27: Digitally measuring the distance and angle
Took a picture from the top to measure the angles

## Slide 28: Digitally measuring the distance and angle
Took a picture from the top to measure the angles
Took a picture on the camera to measure the distance

## Slide 29: Digitally measuring the distance and angle
Measured 4 points for each beam
Extremely high precision
Derivation of error
mm (varied for each measurement)

## Slide 30: Inclining the sensor to prevent a ”stretched” image

## Slide 31: Fitting depth, using refractive index from Brewster’s angle
Fit values:
D
Chart: Angle [˚]
| 10.9135820189679 | 17.8608396520885 | 26.80865253986228 | 31.43674980580048 | 35.39139143031578 | 39.78373205192988 | 45.4255928394796 | 50.7657022145458 | 52.91772421754995 | 57.33763961542578 | 63.50535435756738
Gnuplot fit | 2.6526 | 4.3596 | 6.5947 | 7.7694 | 8.7827 | 9.9161 | 11.377 | 12.7511 | 13.2978 | 14.3975 | 15.8472
Measured data | 3.0467 | 4.6714 | 6.8078 | 7.8947 | 8.8438 | 9.8433 | 11.1217 | 12.3971 | 13.0467 | 14.3489 | 16.2798
Some points are slightly off
Input values:
Index o

## Slide 32: Comparing predicted vs. measured data
Chart: Angle [˚]
| 10.9135820189679 | 17.8608396520885 | 26.80865253986228 | 31.43674980580048 | 35.39139143031578 | 39.78373205192988 | 45.4255928394796 | 50.7657022145458 | 52.91772421754995 | 57.33763961542578 | 63.50535435756738
Uncorrected | 2.507 | 4.1156 | 6.211 | 7.3057 | 8.2453 | 9.2908 | 10.6285 | 11.8754 | 12.3682 | 13.3533 | 14.6387
Measured data | 3.0467 | 4.6714 | 6.8078 | 7.8947 | 8.8438 | 9.8433 | 11.1217 | 12.3971 | 13.0467 | 14.3489 | 16.2798
All points are off
Input values:
D
Index of refraction
Micrometer value

## Slide 33: In search for an explanation

## Slide 34: What if the sides are inclined?
Side 1
Side 2

## Slide 35: What if the sides are inclined?
Side 1
Side 2
Introduce an inclination angle

## Slide 36: Inclination of the sides of sheet of glass

## Slide 37: Reflections: 3D plot
Angle
Camera distance (mm)
Measured beam distance (mm)
Input values:
Index of refraction
Fit Values:
mm
Micrometer:
mm

## Slide 38: Measurement vs. theory correlation
Chart: Measured distance (mm)
| 3.0467177496236 | 4.671408815981738 | 6.807757129241453 | 7.894682352729313 | 8.84384293536507 | 9.843315507022083 | 11.1217344676039 | 12.39706934574315 | 13.04667922252315 | 14.34891035150015 | 16.27984684173429
 | 3.011 | 4.6265 | 6.7719 | 7.8728 | 8.8352 | 9.804 | 11.0767 | 12.426 | 13.0466 | 14.4341 | 16.2863

## Slide 39: Limitations of reflections method: phase diagram
Chart: Refractive index
Suitable for measurement
Unsuitable for measurement

## Slide 40: Internal reflections: conclusion
Usage: | Thickness Inclination angle
Error: | ± 0.005mm ± 0.002˚
Limitation (n = 1.5): | 0.16mm

## Slide 41: Measuring thickness using Michaelson interferometer

## Slide 42: Michelson interferometer
Interference pattern
Half-translucent mirror
Glass sheet
Negative lens
Laser
Inclination of glass sheet causes difference in OPL
Shift of interference pattern (by N stripes)
Notes: OPL = optical path length

## Slide 43: Michelson interferometer: measurement output
[Deepak N. Iyer , Lehigh University, A Michelson interferometric technique for measuring refractive index of sodium zinc tellurite glasses]
Shift of interference pattern by N stripes
Sheet width
Refractive index
Observed pattern
n or d can be obtained by regression

## Slide 44: Michelson interferometer: measuring thickness by regression
Chart: Inclination of glass sheet [°]
| -5.6621374255883E-15 | 1.999999999999994 | 3.600000000000003 | 3.9 | 4.699999999999997 | 5.4 | 5.999999999999995 | 6.4 | 6.999999999999995 | 7.199999999999997 | 7.699999999999997 | 8.100000000000003 | 8.500000000000001 | 9.200000000000001 | 9.500000000000001 | 10.0
meranie | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15
fit | 0 | 0.63724 | 2.0661 | 2.4252 | 3.5241 | 4.6546 | 5.7494 | 6.5441 | 7.8335 | 8.2894 | 9.4862 | 10.5025 | 11.5714 | 13.5689 | 14.4746 | 16.0505
Fit Values:
mm
Micrometer:
mm
Input values:
Index of refraction

## Slide 45: Michelson interferometer: conclusion
Usage: | Thickness
Error: | ± 0.043mm
Limitation (n = 1.5): | (0.3 – 2)mm
Interference pattern
Half-translucent mirror
Glass sheet
Laser
Inclination of glass sheet causes difference in OPL
Shift of interference pattern (by N stripes)

## Slide 46: Back to the definition of the problem…
✓
Invent and construct an optical device that uses a laser pointer and allows contactless determination of thickness, refractive index, and other properties of a glass sheet.

## Slide 47: Observing internal tension

## Slide 48: Observing internal tension
Crossed
polarizers
Glass sheet
Paper

## Slide 49: Observing internal tension: plastic protractor
No object inserted
No change of polarization
Object with an internal tension
Change of polarization

## Slide 50: Observing internal tension: plastic protractor

## Slide 51: Observing internal tension: sheet of glass
No object
Glass sheet
Extremely low internal tension

## Slide 52: Applying external force to create internal tension
Relaxed
Stressed

## Slide 53: Applying external force to create internal tension
Relaxed
Stressed

## Slide 54: Measuring absorption coefficient

## Slide 55: Measuring the absorption coefficient
1.
2.
3.
4.
CMOS
CMOS
CMOS
CMOS

## Slide 56: Measuring the absorption coefficient
Glass sheets
CMOS
reflections
Fresnel’s equations

## Slide 57: Measuring the absorption coefficient
Chart: Sheet width [m]
| 0.0 | 0.0057 | 0.00775 | 0.01345
 | 55.9913 | 22.9913 | 15.8826 | 6.6826

## Slide 58: Absorption: conclusion
Usage: | Absorption
Error: | ± 2m-1
Limitation: | 
Approximated limitation: | 
Usage: | Absorption
Error: | ± 2m-1
Limitation: | 
Approximated limitation: | 

## Slide 59
Refractive index
Thickness
Absorbtion
Internal tension
Contactless calliper

## Slide 60
Refractive index
Thickness
Absorbtion
Internal tension
Contactless calliper

## Slide 61
Refractive index
Thickness
Absorbtion
Internal tension
Contactless calliper

## Slide 62
Refractive index
Thickness
Absorbtion
Internal tension
Contactless calliper

## Slide 63
Refractive index
Thickness
Absorbtion
Internal tension
Contactless calliper

## Slide 64: Output
Quantity | Uncertainty | Range | Method
Index of refraction | ± 0.008 | 0.16mm | Brewster angle
Thickness | ± 0.005mm | 0.16mm | Internal reflections
Inclination angle | ± 0.002˚ | 0.16mm | Internal reflections
Absorption | ± 2m-1 |  | Absorption
Quantity | Uncertainty | Range | Method
Index of refraction | ± 0.008 |  | Brewster angle
Thickness | ± 0.005mm |  | Internal reflections
Inclination angle | ± 0.002˚ |  | Internal reflections
Absorption | ± 2m-1 |  | Absorption

## Slide 65
Refractive index

## Slide 66
Thickness

## Slide 67
Internal tension

## Slide 68
Absorbtion

## Slide 69: Appendix

## Slide 70: Deriving minimal

## Slide 71: Complex index of refraction
Refraction
Absorption
Absorption coefficient
Wavenumber
Notes: Wavelength = 635nm

## Slide 72: Speed of light
Speed of light in the glass
Speed of light in vacuum
Index of refraction

## Slide 73: 2nd method of measuring the index of refraction: Intensity of p-polarized reflected light
Chart: Reflectance of p-polarized light, 𝑛 = 1.49
| 61.04157322490075 | 60.2931198235728 | 59.15876259007464 | 57.84585602887324 | 57.10748112121095 | 55.89174669470412 | 54.65729237438342 | 53.59377321676873 | 52.50149194789974 | 51.60605149843884 | 50.75497122167152
 | 0.0029382 | 0.002567 | 0.0012155 | 0.00057898 | 0.00013724 | 3.8784e-05 | 0.00023456 | 0.00054928 | 0.00090929 | 0.0022615 | 0.002494
 | 0.0024742 | 0.0023116 | 0.0021531 | 0.0019988 | 0.0018488 | 0.0017032 | 0.0015623 | 0.0014262 | 0.0012951 | 0.001169 | 0.0010483 | 0.00093313 | 0.00082359 | 0.00071992 | 0.0006223 | 0.00053094 | 0.00044603 | 0.00036779 | 0.00029643 | 0.00023217 | 0.00017523 | 0.00012584 | 8.4244e-05 | 5.0676e-05 | 2.5387e-05 | 8.63e-06 | 6.6572e-07 | 1.761e-06 | 1.2189e-05 | 3.2231e-05 | 6.2175e-05 | 0.00010231 | 0.00015295 | 0.0002144 | 0.00028697 | 0.00037099 | 0.00046679 | 0.00057473 | 0.00069513 | 0.00082838 | 0.00097483 | 0.0011349 | 0.0013089 | 0.0014972 | 0.0017004 | 0.0019187 | 0.0021527 | 0.0024027 | 0.0026692 | 0.0029527
Fresnel: 56.18˚
Brewster: 56.47˚

## Slide 74: Observing internal tension
pol.
Sheet
pol.
paper

## Slide 75: All data
Fit values:
D
Index o
Chart: Angle [˚]
| 10.9135820189679 | 17.8608396520885 | 26.80865253986228 | 31.43674980580048 | 35.39139143031578 | 39.78373205192988 | 45.4255928394796 | 50.7657022145458 | 52.91772421754995 | 57.33763961542578 | 63.50535435756738
Gnuplot fit | 2.6526 | 4.3596 | 6.5947 | 7.7694 | 8.7827 | 9.9161 | 11.377 | 12.7511 | 13.2978 | 14.3975 | 15.8472
Uncorrected | 2.507 | 4.1156 | 6.211 | 7.3057 | 8.2453 | 9.2908 | 10.6285 | 11.8754 | 12.3682 | 13.3533 | 14.6387
Corrected | 2.9838 | 4.6107 | 6.7672 | 7.8757 | 8.843 | 9.8265 | 11.115 | 12.4642 | 13.0769 | 14.4349 | 16.2445
Measured data | 3.0467 | 4.6714 | 6.8078 | 7.8947 | 8.8438 | 9.8433 | 11.1217 | 12.3971 | 13.0467 | 14.3489 | 16.2798
Actual Values:
mm

## Slide 76: Fiting thickness and inclination angle
Chart: Angle-distance relation based on index of refraction and depth of glass sheet
| 10.9135820189679 | 17.8608396520885 | 26.80865253986228 | 31.43674980580048 | 35.39139143031578 | 39.78373205192988 | 45.42559283947958 | 50.7657022145458 | 52.91772421754997 | 57.33763961542578 | 63.50535435756738
 | 3.0467 | 4.6714 | 6.8078 | 7.8947 | 8.8438 | 9.8433 | 11.1217 | 12.3971 | 13.0467 | 14.3489 | 16.2798
 | 3.011 | 4.6265 | 6.7719 | 7.8728 | 8.8352 | 9.804 | 11.0767 | 12.426 | 13.0466 | 14.4341 | 16.2863
Perfect fit!
Camera distance values unique for each point

## Slide 77: Michelson interferometer: measuring refractive index by regression
Chart: Inclination of glass sheet [°]
| -5.6621374255883E-15 | 0.999999999999994 | 2.300000000000005 | 2.499999999999994 | 3.100000000000003 | 3.499999999999994 | 4.100000000000001 | 4.300000000000006 | 4.6 | 5.100000000000001 | 5.199999999999997 | 5.499999999999995 | 5.699999999999997 | 5.800000000000006 | 6.100000000000001
meranie | 0 | 2 | 4 | 6 | 8 | 10 | 12 | 14 | 16 | 18 | 20 | 22 | 24 | 26 | 28
fit | 0 | 0.74449 | 3.9397 | 4.655 | 7.1594 | 9.1281 | 12.5305 | 13.7847 | 15.7785 | 19.4025 | 20.1725 | 22.573 | 24.2488 | 25.1093 | 27.7819
Fit Values:
Brewster’s angle:
Input values:
mm