## Slide 1: Problem № 9 Salt Production
Reporter: Saba Gogichaishvili
Team: Georgia

## Slide 2: Problem
Solar evaporation of seawater or salt mining are common methods to produce common salt (NaCl). Propose a method to extract salt from natural source and determine both productive capacity of your method and purity of the product. Demonstrate an amount of salt produced by your method.

## Slide 3: Plan
Theoretical model
  Seawater composition
  Samples theoretical composition
  Theoretical salt quantity
Experiments
  Measuring samples composition
  Extracting salt
  Determining obtained salt quantity
Conclusion

## Slide 4: Theoretical model

## Slide 5: Seawater composition
Chart: 
| Water | Solid
 | 965 | 35
Chart: 
| Cl | Na | SO4 | Mg | Ca | K | HCO3 | Other Ions (Sr, Ba,...)
 | 0.55 | 0.306 | 0.077 | 0.037 | 0.012 | 0.011 | 0.004 | 0.003

## Slide 6: Samples theoretical composition (based on salinity measurements in nature)
C(E) = ω(E) * salinity‰ * 10 mg/L
C(E) – Element concentration in sample
ω(E) – Percentage of element in salt

## Slide 7: Sample № 7
Chart: Salinity = 12.9 ‰
| Na | K | Ca | Mg | Cl | SO4 | HCO3
 | 3974 | 142 | 155 | 477 | 7095 | 993 | 52

## Slide 8: Sample № 8
Chart: Salinity = 12.2 ‰
| Na | K | Ca | Mg | Cl | SO4 | HCO3
 | 3733 | 134 | 147 | 451 | 6710 | 939 | 49

## Slide 9: Sample № 9
Chart: Salinity = 15.2 ‰
| Na | K | Ca | Mg | Cl | SO4 | HCO3
 | 4552 | 169 | 177 | 562 | 8360 | 1167 | 61

## Slide 10: Measuring samples composition
Component | Measurement method
Na+, K+ | Flame emission spectroscopy
Ca2+, Mg2+ | Complexometric titration
Cl – | Silver nitrate titration with chromate indicator (Mohr’s method)
HCO3– | Alkalimetric titration
SO42– | Turbidimetry
Sedimented particles | Turbidimetry

## Slide 11: Flame emission spectroscopy (Na+, K+)

## Slide 12: Na
Chart: 
| 0 | 0.2 | 1 | 2 | 5 | 10 | 20
Intensity | 0 | 1.1 | 3.7 | 6 | 10.8 | 15.6 | 21.9
Chart: 
| 0 | 0.5 | 1 | 2 | 3 | 4 | 5
Intensity | 0 | 3.3 | 6.2 | 11.8 | 16.3 | 20.4 | 23.9
K

## Slide 13: Complexometric titration Ca2+, Mg2+
xide Blue purple (pH=11.3)
xide-Calcium complex Red (pH=11.3)
(Eriochrome black T, Solochrome black T) Blue (pH=10)
+ H+
+ M2+

## Slide 15
Sample № | V (ml) | V1 (ml) | V2 (ml) | C (Ca) mg/l | C (Mg) mg/l
7 | 5 | 4,3 | 23,2 | 172 | 454
8 | 5 | 4,2 | 21,5 | 168 | 415
9 | 5 | 5 | 27,4 | 200 | 538

## Slide 16: Silver nitrate titration with chromate indicator (Mohr's method) (Cl –)
Cl– + Ag+  AgCl↓
2Ag+ + CrO42–  Ag2CrO4↓(Orange)

## Slide 17
Sample № | V (ml) | V1 (ml) | C (Cl) mg/l
7 | 1 | 2,00 | 7 100
8 | 1 | 1,92 | 6 816
9 | 1 | 2,36 | 8 378

## Slide 18: Alcalimetric titration (HCO3–)
H+ + – H2O + CO2↑

## Slide 19
Sample № | V (ml) | V1 (ml) | C () mg/l
7 | 100 | 2,86 | 174
8 | 100 | 2,78 | 169
9 | 100 | 3,04 | 185
Sample № | V (ml) | V1 (ml) | 
7 | 100 | 2,86 | 174
8 | 100 | 2,78 | 169
9 | 100 | 3,04 | 185

## Slide 20: Turbidimetry (Sedimented particles & SO42–)
Ba2+ + SO42–  BaSO4↓
Also, some Etilenglicol (CH2OH)2 is added for even distribution of precipitate

## Slide 21: Results
Sample № | C (SO4) mg/l
7 | 1 540
8 | 1 400
9 | 2 100

## Slide 22: T0,C0 – Before filtration T , C – After filtration
Sample № | T0 FTU | T FTU | C0 mg/l | C mg/l
7 | 644 | 110 | 412.16 | 70.4
8 | 466 | 66 | 298.24 | 42.24
9 | 548 | 137 | 350.72 | 87.68
Samples were filtrated by 0.45μ filter
FTU - Formazin Turbidity Unit

## Slide 23: Sample №7
Chart: Concentration mg/l
| Na | K | Ca | Mg | Cl | SO4 | HCO3
 | 3850 | 149 | 172 | 454 | 7100 | 1540 | 174

## Slide 24: Sample №8
Chart: Concentration mg/l
| Na | K | Ca | Mg | Cl | SO4 | HCO3
 | 3630 | 143 | 168 | 415 | 6816 | 1400 | 169

## Slide 25: Sample №9
Chart: Concentration mg/l
| Na | K | Ca | Mg | Cl | SO4 | HCO3
 | 4390 | 165 | 200 | 538 | 8378 | 2080 | 185

## Slide 26: Extracting salt
Bringing crucibles to constant weight & weighting them
Taking 100ml of each water sample & evaporating them
Bringing obtained salt to constant weight

## Slide 27: Bringing crucibles to constant weight & weighting them

## Slide 28: Taking 100ml of each water sample & evaporating them

## Slide 30: Determining obtained salt quantity M (salt) = M - M0
Sample № | M0 g | M g | M (salt) g
7 | 69,4158 | 70,7116 | 1,2958
8 | 69,6125 | 70,8504 | 1,2379
9 | 68,1200 | 69,7627 | 1,6427

## Slide 31: Conclusion
Comparing theoretical and experimental salt quantities
Comparing theoretical and experimental salt compositions

## Slide 32: Comparing theoretical and experimental salt quantities
Chart: 
| 7 | 8 | 9
Theoretical | 1.29 | 1.22 | 1.52
Experimental | 1.296 | 1.238 | 1.643

## Slide 33: Sample №7 Element concentrations
Chart: Concentration mg/l
| Na | K | Ca | Mg | Cl | SO4 | HCO3
Theoretical | 3947 | 142 | 155 | 477 | 7095 | 993 | 52
Experimental | 3850 | 149 | 172 | 454 | 7100 | 1540 | 174

## Slide 34: Sample №8 Element concentrations
Chart: Concentration mg/l
| Na | K | Ca | Mg | Cl | SO4 | HCO3
Theoretical | 3733 | 134 | 147 | 451 | 6710 | 939 | 49
Experimental | 3630 | 143 | 168 | 415 | 6816 | 1400 | 169

## Slide 35: Sample №9 Element concentrations
Chart: Concentration mg/l
| Na | K | Ca | Mg | Cl | SO4 | HCO3
Theoretical | 4552 | 169 | 177 | 562 | 8360 | 1167 | 61
Experimental | 4390 | 165 | 200 | 538 | 8378 | 2080 | 185

## Slide 36: References
Na, K determination – ISO 9964-3:1993
Ca, Mg determination – ISO 6058-84, ГОСТ 23268.5-78
Cl determination – ISO 9297-89
SO4 determination – ГОСТ 4389-72
HCO3 determination – ГОСТ 23268.3-78
Sedimented particles – ISO 7027-99
Evaporation – ГОСТ 18164-72

## Slide 37: Thanks for your attention